Magnetism and Magnetic Materials

Magnetic Properties of Ferromagnetic-Insulator Composites
Shchotkin V.V., Pazukha I.M.
Department of Electronics, General and Applied Physics, Sumy State University, 2, Rymsky Korsakov Str., 40007 Sumy, Ukraine
E-mail: v.shchotkin@aph.sumdu.edu.ua

   As a rule, detailed information about the magnetic state of ferromagnetic-insulator composites is basically obtained from their magnetic measurements while using SQUID (temperature range 5-300 K) or vibrating magnetometers (with temperature range 90-300 K) in steady magnetic field up to 1 T.
   It was established that the magnitude of the coercive force Вс observed in (Fe50Co50+SiO2)/S composites does not exceed value 1.8 mT in the concentration range of the magnetic component х = 51-80% and reaches its minimum value of 0.78 mT at х = 59.7%. The process of thermal annealing will lead to an increase in both the saturation magnetization and the magnetic susceptibility as well.
     The detailed analysis of magnetization curves showed that their shape and the magnetic parameters (coercive force, saturation magnetization, residual magnetization, and saturation field) also strictly depend on the Co concentration and the measurement temperature. It should also be noted that according to investigations of the magnetization curves for “in-plane” magnetization at room temperature for granular films, all composite structures can be divided into three groups depending on ferromagnetic material concentration.
      Much lower the percolation threshold (х < 40 mol.%), the magnetization curves are correspond to the superparamagnetic state. The shape and slope of the curve near magnetic fields with zero value mostly depend on the ferromagnetic material concentration and the measurement temperature. In the concentration range of 44 < x < 61mol.%, the magnetization curves have a characteristic slope in small applied fields, that almost independent of Co concentration and temperature.
   For higher concentrations (х > 61 mol.%), the magnetization curves retain their linearity and all characteristic features of "hard" magnetization, but the effective field of perpendicular anisotropy with increasing Co concentration will be decreased. Considering that in this concentration range the transition of a granular system through the percolation threshold occurs, the corresponding change in the value of perpendicular anisotropy is associated with an increase in intergranular interaction, which forms a collective state, whose magnetic properties begin to dominate the properties of individual granules.
     This work was funded by the State Program of the Ministry of Education and
Science of Ukraine 0119U100777 (2019-2021).