Nanocomposites and nanomaterials

Nanoporous metals, neat and modified by porous substances, as an “inverted” alternative to discrete nanostructures
Lytvynenko A.S.1,2
1 Porous Compounds and Materials Dept., L. V. Pisarzhevsky Institute of Physical Chemistry of the NAS of Ukraine. Prospect Nauky, 31, Kyiv, 03028, Ukraine.
E-mail: anton.s.lytvynenko@gmail.com
2 Jagiellonian University, Faculty of Chemistry, Gronostajowa 2, 30-387 Kraków, Poland

Metal nanoparticles, both neat and supported on porous carriers, are well established tool for various applications. However, a number of aspects of their utilization are impaired by their discrete nature: electrochemical (connection to circuit must be ensured), catalytic (necessity of filtering off) properties, deposition of coatings (binding agent is to be added) etc. Nanofoams (NFs), resulting from electrochemical deposition of the metals accompanied by H2 evolution [1], can be an attractive alternative. The work aimed at evaluating prospects of utilization of the nanofoams and their modification by porous substances by different means.
Ag, Cu, Sn NFs were prepared following the procedures developed by us or similar to reported elsewhere [1-2]. Ag NF revealed higher electrocatalytic activity in reductive dehalogenation of a set of organic halides [1], influence of the deposition conditions on the nanofoam structure and its activity in bromobenzene debromination was elucidated. Ag and Cu NFs were successfully modified by dropcasting of metal-organic frameworks (MOFs) particles, opening a way to NF-supported MOF catalysts. Sn NF was modified by SnOx via thermal and anodic oxidation [2] (which differently impacted the wetting behavior of the foam). The works were partially supported by Visegrad Scholarship (contract #51810453) and grant for Projects of Young Scientists of the NAS of Ukraine (#69-09/06-2020).

1. Mishura A. M., Lytvynenko A. S., Gavrilenko K. S., Baranchikov A. E., Grabovaya N. V., Kiskin M. A., Kolotilov S. V. Formation of hierarchically-ordered nanoporous silver foam and its electrocatalytic properties in reductive dehalogenation of organic compounds // New J. Chem. - 2018. - 42. - P. 17499–17512.
2. Gurgul M., Lytvynenko A.S., Jarosz M., Gawlak K., Sulka G.D., Zaraska L. Hierarchical Nanoporous Sn/SnOx Systems Obtained by Anodic Oxidation of Electrochemically Deposited Sn Nanofoams // Nanomater. - 2020. - 10. - 410.