Nanocomposites and nanomaterials

Composites of Pd nanoparticles and nanoporous anodic tin oxide
Lytvynenko A.S.1,2, Gawlak K.2, Zaraska L.2, Kolotilov S.V.,1 Sulka G.D.2
1 Porous Compounds and Materials Dept., L. V. Pisarzhevsky Institute of Physical Chemistry of the NAS of Ukraine. Prospect Nauky, 31, Kyiv, 03028, Ukraine.
E-mail: anton.s.lytvynenko@gmail.com
2 Jagiellonian University, Faculty of Chemistry, Gronostajowa 2, 30-387 Kraków, Poland

Nanostructured Pd, typically deposited on various porous supports, is an essential material for various catalytic reactions in fine organic synthesis industry, including C-C coupling reactions [1], hydrogenation processes etc. As a convenient way for improving reproducibility of such composite characteristics, simplifying the catalyst separation from the products as well as adaptation of the former to processes in flow mode, we propose to impregnate Pd into nanoporous oxide layers obtained via electrochemical oxidation of tin.
The aim of the work is to elucidate possibility of creation of nanocomposites by impregnation of tin oxide nanopores by a Pd salt followed by reduction of the latter as well as to characterize structure of such composites.
Porous SnOx layers with quasi-cylindrical pores (with diameters of dozens of nm) aligned normally to the layer surface were grown on Sn foil using anodic oxidation of the latter in aqueous NaOH [2]. The impregnation was performed by immersing the material into solutions containing various concentrations of [PdCl4]2- for 1–15 min. It was found that SnOx reduced [PdCl4]2- to Pd0 without any additional reducers, allegedly via Sn2+ ions. The SnOx structure acted as a template for the deposition of the nanoparticles formed as “plugs” closing the pores.
The work was supported by Queen Jadwiga Scholarship granted to A.S.L. in 2019/2020 academic year.

1. Shang N., Gao Sh., Zhou X., Feng Ch., Wang Zh., Wang Ch. Palladium nanoparticles encapsulated inside the pores of a metal–organic framework as a highly active catalyst for carbon–carbon cross-coupling // RSC Adv. - 2014. - 4. - P. 54487-54493.
2. Zaraska L., Gawlak K., Wiercigroch E., Malek K., Kozieł M., Andrzejczuk M., Marzec M.M., Jarosz M. Brzózka A., Sulka G.D. The effect of anodizing potential and annealing conditions on the morphology, composition and photoelectrochemical activity of porous anodic tin oxide films // Electrochim. Acta. - 2019. - 319. - P. 18-30.