Nanostructured surfaces

Self-organized femtosecond laser-induced periodic surface structures on silicon
Karlash A.1 Dmitruk I.2,3, Hraboskyi E.2, Dmytruk A.3, Blonskyi I.3
1 Faculty of Radiophysics, Electronics and Computer Systems, Taras Shevchenko National Uniersity. of Kyiv, Kyiv 01601, Ukraine.
E-mail: anna_karlash@ukr.net
 2 Faculty of Physics, Taras Shevchenko National University of Kyiv, Kyiv 01601, Ukraine.
3 Institute of Physics, National Academy of Sciences of Ukraine, Kyiv 03028, Ukraine.

Micro- and nanostructuring on different crystallographic orientation surfaces of silicon, both n- and p-types, have been obtained by irradiation with a number of space-time shifted pulses of Ti: sapphire femtosecond laser. The laser ablation leads to the patterning of the silicon surface with laser-induced periodic surface structures (LIPSS). The laser pulses with a wavelength of 800 nm, pulse energy of 1,44 mJ and repetition rate of 1 kHz were focused on the surface with a cylindrical lens. The polarized laser beam with the energy density of 0.08–0.14 J/cm2 falls normally on the sample surface in air environment. Movement of the sample at a constant velocity from 0.5 to 0.9 mm/s during the irradiation provided processing of a large surface area. SEM images of the Si surface treated by the laser radiation with the energy density of 0.1 J/cm2 are presented in the Figure for different types of the laser beam polarization: (a) horizontal; (b) vertical; (c) circular. In the case of linear polarization the orientation of the LIPSSs is perpendicular to the laser beam polarization, the period of the formed LIPSSs is about 550-570 nm. In the case of circular polarization a granular surface structure has been formed with the mean diameter of 2-3 µm. We also observed small nanoparticles, presumably, of Si or partially oxidized, with diameter about 10 nm deposited on the surface of the granules during laser ablation process. Furthermore, smaller period LIPSS formed by the second and the third laser harmonics are under investigation.