Nanostructured surfaces

Self-Assembled Rare-Earth Nanostripe Arrays in the Ce/Mo(112) System
Afanasieva T.V.1, Fedorus A.G.1, Goriachko A.M.1,2, Naumovets A.G.1, Neporozhniy I.N.1,2 , Rumiantsev D.V.1
1 Physical Electronics Department, Institute of Physics of the NAS of Ukraine. Prospect Nauki, 46, Kyiv-03039, Ukraine.
E-mail: andreandy2000@gmail.com
2 Taras Shevchenko University of Kyiv, Glushkova Avenue 4G, Kyiv-03187, Ukraine.

We report investigation results of submonolayer Ce films on the Mo(112) surface by means of low energy electron diffraction (LEED) and density functional theory (DFT) calculations. The equilibrium structure for Ce coverages θ < 0.5 is found to be a regular array of [110] oriented nanostripes, which are placed at regular mesoscopic intervals along the [111] direction of the Mo(112) substrate. A comprehensive investigation of the nanostripe phase by LEED and other comlementary experimental surface science techniques indicates that they consist of a single atomic monolayer p(21)-Ce/Mo(112) superstructure with up to 20% oxygen impurity. The mesoscopic array periodicity is found to be in the range from ~ 6 nm to infinity, while each nanostripe’s width varies from ~ 3 nm to infinity, depending on θ and surface preparation conditions.
The DFT simulation has revealed: (1) The linear structure of single Ce chains on the Mo(112) surface is energetically favourable over zigzag chains; (2) Formation of the second linear chain next to the first one at a distance of 0.546 nm is energetically favoured over placement at 0.38 nm distance or anywhere in the uncovered area of the Mo(112). In this case, Ce atoms shift and rearrange into a zigzag structure with interatomic distances of 0.525 nm in the [111] direction. The placement of Ce atoms at distances shorter than 0.546 nm indicates the presence of a strong attraction between the chains of Ce atoms on Mo(112). The presence of O atoms stabilizes the p(21) adlayer superstructure within the stripes, instead of the c(22) in atomically pure Ce/Mo(112) system [1]; (3) Formation of Ce islands leads to appearance of surface stress, such that the chains of the adsorbate tend to compress, and the substrate under the adsorbate tends to slightly stretch.

Godzik G., Pfnür H., Lyuksyutov I. F. Impurity-induced changes of overlayer symmetry and of phase transitions // Europhys. Lett.-2001.-56.-P. 67-73.