### Nanostructured surfaces
The effect of annealing on the characterizations of the grain-boundary of silicon films

Rodionova T.V.

Faculty of Radio Physics, Electronics and Computer Systems, Taras Shevchenko National University of Kyiv, Volodymyrska Street 64, 01033, Kyiv 33, Ukraine
E-mail: rodtv@univ.kiev.ua

It is known that the structure of silicon films determines their electrophysical, optical, and other properties, which is important in terms of their practical application in microelectronics, solar energy, spintronics. The important element of the film structure is grain boundaries. The characteristics of grain boundaries are determined by film formation conditions and subsequent treatments, in particular, annealing.
In this paper, we analyzed the types of grain boundaries and grain boundaries joints, and estimated the relative energy of grain boundaries in phosphorus-doped silicon films depending on the temperature and annealing time.
Silicon films were prepared by low-pressure chemical vapour deposition on thermally oxidized (100 nm oxide thickness) (100) Si wafers. The deposition temperature was equal to 6300C. The film thickness was 500 nm. Samples were doped with phosphorus (1021 cm-3). Films were annealed for 30 min and 3 hours in a nitrogen atmosphere at a temperature ranging from 9500C to 12000C. The relative grain-boundary energy was determined by the method of grain boundary grooves with the use of atomic force microscopy. This method is described in [1] in detail.
It was found that with increasing annealing temperature the number of low energy special grain boundaries and joints of grain boundaries increases and the number of high energy general-type boundaries decreases. In addition, faceting of grain boundaries takes place under annealing. These processes lead to a decrease in the relative energy of grain boundaries. The highest value of the relative grain-boundary energy was observed for as-deposited films. The smallest values were observed in films that were annealed at 11500С.

[1] Rodionova T.V., Lytvyn P.M. Estimation of the relative energy of grain boundaries in silicon films by the of grain boundary grooves method // J. Nano- Electron. Phys. - 2018. - 10, No 6. - P. 06040-1 – 06040-4.