Physico-Chemical nanomaterials science

Influence of substituents on photoresponsive behavior of methacrylic polymers containing 8-hydroxy-quinoline azo-dyes in side-chain
D. Chomickia, O. Kharchenkob, A. Kozanecka-Szmigielc, D. Szmigield,
Ł. Skowrońskie, J. Kowalonekf, V. Smokalb, O. Krupkab,
B. Derkowska-Zielinskaa
a Faculty of Physics, Astronomy and Informatics, Nicolaus Copernicus University in Torun, Grudziadzka 5, 87-100 Torun, Poland
e-mail: chomicki@doktorant.umk.pl
b Faculty of Chemistry, Taras Shevchenko National University of Kyiv,
Volodymyrska 60, 01033 Kyiv, Ukraine
c Faculty of Physics, Warsaw University of Technology,
75 Koszykowa Str., 00-662 Warsaw, Poland
d Sieć Badawcza Łukasiewicz – Instytut Technologii Elektronowej,
Al. Lotnikow 32/46, 02-668 Warsaw, Poland
e Institute of Mathematics and Physics, UTP University of Science and Technology,
S. Kaliskiego 7, 85-796 Bydgoszcz, Poland
f Faculty of Chemistry, Nicolas Copernicus University in Torun,
Gagarina 7, 87-100 Torun, Poland

In recent years, azobenzene-containing materials receive much scientific attention due to their optoelectronic properties, which make them attractive for such applications as optical data storage, optical switching, signal processing, nonlinear optical devices and many more. Azobenzene is constituted of two phenyl rings linked by an azo (–N=N–) bridge. It can appear in two isomeric forms (stable trans and metastable cis) with different spectroscopic properties and that makes reversible trans-cis photoisomerization one of its important features [1]. When the azobenzene molecules embedded into polymer matrix are excited with linearly polarized light, after they go through multiple the trans→cis→trans cycles, they tend to align in such a way that the long axis of the molecule is perpendicular to the polarization direction. This allows to orient the molecules with light only and below the glass transition temperature of a polymer. As a consequence, birefringence and dichroism are induced in the material [2].
Spectroscopic properties as well as isomerization quantum yields and thermal relaxation rate of azobenzenes can be tailored by introducing various electron donating/withdrawing substituents into the molecule and/or by the change in molecular structure. Understanding of a relationship between the structure and properties of azobenzene derivatives is crucial for designing materials suited for specific applications.
In this study we present optical properties of a novel class of methacrylic polymers containing 8-hydroxy-quinoline azo-dyes in side-chain. The goal of our study was to examine the influence of various substituents in the chromophores on the complex refractive index of the material and the ability to form surface relief gratings.

1 B. Derkowska-Zielinska et. al, Optical Materials, 2018, 85, 391-398.
2 B. Derkowska-Zielinska et. al, Journal of Physical Chemistry C, 2020, 124, 939-944.