Physico-Chemical nanomaterials science

Inhibition of steel corrosion with imidazolium-based compounds - experimental and theoretical study
Legut D.1, Kądzielawa A. P.1,2, Pánek P.3,4, Marková K.5, Váňová P.5, Konečná K.5, and Langová Š.5
1 IT4Innovations, VŠB-Technical University of Ostrava, 17. listopadu 2172/15, 708 00 Ostrava-Poruba, Czech Republic
2 Instyut Fizyki Teoretycznej, Uniwersytet Jagielloński, ul. Łojasiewicza 11, 30-348 Kraków, Poland
3 Faculty of Materials Science and Technology, VŠB-Technical University of Ostrava, 17. listopadu 2172/15, 708 00 Ostrava, Czech Republic
4 Institute of Environmental Technology, VŠB-Technical University of Ostrava, 17. listopadu 2172/15, 708 00 Ostrava, Czech Republic
5 Faculty of Materials Science and Technology, VŠB-Technical University of Ostrava, 17. listopadu 2172/15, 708 00 Ostrava, Czech Republic.

We investigate the inhibition of corrosion of the mild steel by 1-octyl-3-methylimidazolium hydrogen sulfate, 1-butyl-3-methylimidazolium hydrogen sulfate, and 1-octyl-3-methylimidazolium chloride, using electrochemical, weight loss, and surface analysis methods as well as the full quantum-mechanical treatment. The inhibition efficiency obtained from the polarization curves is about 80-92% for all of the 1-octyl-3-methylimidazolium salts with a concentration higher than 0.005 mol/l, while it is much lower for 1-butyl-3-methylimidazolium hydrogen sulfate. The values measured in the weight loss experiments (after seven days) are to some extent higher (reaching up to 98% efficiency). We have shown that the influence of the alkyl chain length on the inhibition efficiency is much more significant than that of the anion type. Furthermore, we obtain a realistic model of a single molecule on iron surface Fe(110) by applying the Density Functional Theory calculations. We use the state-of-the-art computational approach, including the meta-GGA to model the electronic structure properties of both free and bounded-to-surface imidazolium-based molecules. This model supports the experimental findings and explains the influence of the alkyl chain length on the inhibition process.
This work was supported by TAČR, project No. FV10089, Synthesis of Ionic Liquids in Microwawe Reactor, by the ERDF in the IT4Innovations National Supercomputing Center Path to Exascale (CZ.02.1.01/0.0/0.0/16_013/0001791) within the OPRDE, the project e-INFRA CZ (ID:90140) by the Ministry of Education, Youth and Sports of the Czech Republic.