Nanocomposites and nanomaterials

Influence of conditions of Ag nanofoam electrodeposition on its performance in preparative debromination of aryl bromides
Lytvynenko A.S.1, Tarasova I.V.1,2, Gavrilenko K.S.3, Kolotilov S.V.1
1 Porous Compounds and Materials Dept., L. V. Pisarzhevsky Institute of Physical Chemistry of the NAS of Ukraine. Prospect Nauky, 31, Kyiv, 03028, Ukraine.
E-mail: anton.s.lytvynenko@gmail.com
2 Department of Inorganic Chemistry, Faculty of Chemistry, Taras Shevchenko National University of Kyiv. Lva Tolstogo str., 12, Kyiv, 01033, Ukraine
3 ChemBioCenter, Taras Shevchenko National University of Kyiv, Chervonotkatska str., 61, 02094, Kyiv, Ukraine

Electrochemical reductive dehalogenation is a prospective tool for remediation of halogen-containing persistent organic pollutants, such as polyhalogenated biphenyls, freons, and inert pesticides [1]. High efficiency of silver nanofoams (NFs) as electrocatalysts of this process was previously shown by us [2]. The aim of the work was to elucidate the influence of the electrodeposition conditions on the performance of the resulting Ag NF in electrochemical dehalogenation of 1-fluoro-4-bromobenzene (FPhBr).
The NFs were deposited from aqueous AgNO3+HBF4 onto glassy carbon varying the concentrations of the components and the deposition time. The debromination of FPhBr was performed in an undivided 3-electrode cell with a Mg sacrificial anode under Ar atmosphere. The variation of the deposition conditions notably changed the sizes of the nanofoam structural elements and slightly influenced the fluorobenzene yield. In particular, the decrease of the [Ag+] in the deposition bath from 0.02 to 0.01 mol/L increased the yield from 41 % to 50 % (at ca. 90% Faradaic efficiency in both cases) at the same debromination conditions at constant potential. The impact could be caused by difference in number and activity of superficial defects on the AgNF surfaces.

1. Martin E.T., McGuire C.M., Mubarak M. S., Peters D.G. Electroreductive Remediation of Halogenated Environmental Pollutants // Chem. Rev. - 2016. - 116. - P. 15198–15234.
2. Mishura A.M., Lytvynenko A.S., Gavrilenko K.S., Baranchikov A.E., Grabovaya N.V., Kiskin M.A., Kolotilov S.V. Formation of hierarchically-ordered nanoporous silver foam and its electrocatalytic properties in reductive dehalogenation of organic compounds // New J. Chem. - 2018. - 42. - P. 17499-17512.