Nanocomposites and nanomaterials

Inelastic internal friction in nanocomposites of multiwalled carbon nanotubes and polyethylene, polyvinyl chloride, expanded polystyrene
Alieksandrov M.A., Onanko A.P., Dmytrenko O.P., Kulish M.P., Onanko Y.A., Charnyi D.V., Shevchuk S.A., Pinchuk-Rugal T.M., Pavlenko O.L. Busko T.O., Kurochka L.І., Ilyin P.P.
Kyiv national university, Volodymyrs’ka str., 64, Kyiv-01601, Ukraine.
E-mail: onanko@i.ua

The transversal US velocity V┴ = 768 ± 30 m/sec, shear modulus G = ρV┴2 = 578 MPa, the longitudinal US velocity V║ = 2485 ± 30 m/sec, dynamical elastic modulus E = ρV║2 = 6,057 GPa, Poisson coefficient μ = 0,44 nanocomposite polyethylene with low density high pressure (C2H4)n + 3% MWCNT were determined from the oscillogram in fig. 1 [1].

Fig. 1. The illustration of the window for processing data of transversal elastic wave velocity measuring V┴ = 768 m/sec in nanocomposite polyethylene + 3% MWCNT by phase method

à

Conclusions
1. 
ис.1 к статье О.В.Ляшенко, А.П.Онанко Влияние электрического тока на упругие и неупругие характеристики Ge0.963Si0.037.

à

The value of internal friction background Q-10 after temperature, mechanical treatments describes the changes of the elastic stress σi fields in nanocomposite.
2. 
ис.1 к статье О.В.Ляшенко, А.П.Онанко Влияние электрического тока на упругие и неупругие характеристики Ge0.963Si0.037.

à

ис.1 к статье О.В.Ляшенко, А.П.Онанко Влияние электрического тока на упругие и неупругие характеристики Ge0.963Si0.037.

à

ис.1 к статье О.В.Ляшенко, А.П.Онанко Влияние электрического тока на упругие и неупругие характеристики Ge0.963Si0.037.

à

The increase of the nanocomposite crystallinity degree at growth of multiwalled carbon nanotubes concentration filling with the nanotubes of matrix results in the decline of content of organized phase.

1.	Onanko A. P., Kuryliuk V. V., Onanko Y. A. et al. Peculiarity of elastic and inelastic properties of radiation cross-linked hydrogels // J. Nano- and Elec. Phys.- 2020.-12, № 4.– P. 4026-4030.
DOI: https://doi.org/10.21272/jnep.12(4).04026.