Nanostructured Surfaces

(Ce+O)/Mo(112) Nanostructured Surface
Goriachko A.1,2, Fedorus A.G.1, Rumiantsev D.V. 1
1 Physical Electronics Department, Institute of Physics of the NAS of Ukraine. Prospect Nauki, 46, Kyiv-03039, Ukraine.
2 Faculty of Radiophysics, Electronics and Computer Systems, National Taras Shevchenko University of Kyiv, Prospect Glushkova 4G, Kyiv-03127, Ukraine.
E-mail: goriachko@knu.ua

Nowadays, there is a strong scientific interest in studying monolayer rare earth oxides on refractory metal substrates [1]. Recently it has been shown that a rare-earth metal Ce co-adsorbed with a small amount of oxygen on the Mo(112) surface leads to intriguing mesoscopic nanostructuring and drastic lowering of the electron work function [2]. In order to clarify the role of oxygen in defining the adsorbate reconstruction, here we focus on the (Ce+O)/Mo(112) interface with comparable concentrations of Ce and O atoms.
We have co-deposited Ce and O by evaporating Ce from an oxygen-containing metallic source onto atomically clean Mo(112) surface with subsequent flash-annealing up to 1400 K. All experiments were performed in an ultra-high vacuum chamber (background pressure in the low 10-11 mbar range). The samples were investigated in-situ by means of low energy electron diffraction (LEED), Auger electron spectroscopy (AES) and electron beam based contact potential difference measurements.
Our observations indicate that for Ce coverage ≈0.6 the high oxygen content causes the formation of the c(4×4) superstructure within the ad-layer as opposed to the c(8×4) superstructure in the case of low oxygen content, which was reported elsewhere [2]. Accordingly, we propose an atomic model of the newly observed interface with oxygen atoms present in every in-plane unit cell of the superstructure and not just at the domain boundaries, resulting in the non-compressed ad-layer. We discuss possible applications in such areas as electron emission, photon-detection, green energy storage, nanobiotechnology, etc.

1. Kuchowicz M., Coadsorption of samarium with oxygen on molybdenum (211) surface // Applied Surface Science.-2010.-256.-P. 4818-4821.
2. Afanasieva T. V., Fedorus A. G., Goriachko A. M. et al, Mesoscopic self-ordering in oxygen-doped Ce films adsorbed on Mo(112) // Surface Science.-2021.-705.-121766.