### Nanostructured surfaces
Formation of special grain boundary joints in phosphorus-doped polysilicon films under annealing

Rodionova T.V.

Faculty of Radio Physics, Electronics and Computer Systems, Taras Shevchenko National University of Kyiv, Volodymyrska Street 64, 01033, Kyiv 33, Ukraine
E-mail: rodtv@univ.kiev.ua

An essential element of the structure of polycrystalline films, together with grain boundaries, are the joints of grain boundaries, that are a kind of linear defects. Joints are of great importance for controlling the properties of materials, that is due to their significant influence on the electrophysical, optical, mechanical and other properties from the point of view of practical applications. Joints are the least studied structural element in polycrystals.
The aim of this work is to study the mechanisms of the formation of special joints of grain boundaries in phosphorus-doped polysilicon films during annealing.
Polysilicon films were obtained by low-pressure chemical vapour deposition on thermally oxidized (100 nm oxide thickness) (100) Si wafers. The deposition temperature was equal to 6300C. The film thickness was 500 nm. The films were doped with phosphorus and annealed at temperatures from 9500C to 12000C. for 30 minutes. The structure of the films was studied by transmission electron microscopy. Surface morphology was analyzed by atomic force microscopy.
It is shown that, the number of special joints (both triple and multiple) increases from 54.8% for as deposited films to 77.5% for films annealed at 11500C.
The most probable mechanism for the formation of special joints of grain boundaries in polysilicon films upon annealing is the splitting of grain boundaries. The initiation of the splitting process occurs in the places where the boundary is distorted. Grain boundaries can split if their misorientation is the sum of rotations that lead to the formation of low-energy boundaries. It is known that multiple twinning is a characteristic feature of the formation of the structure of polysilicon films. The interaction of high-order twins leads to the formation of special joints of grain boundaries. During the grains growth under annealing, random contacts of special boundaries take place, that leads to an increase in the relative number of special joints.