Physico-chemical nanomaterials science

Electrochemical hydrogenation properties of Ni/Co-C composites

Vlad Kh.I.1, Verbovytskyy Yu.V.1, Bogatyrov V.M.2, Zavaliy I.Yu.1

1 Karpenko Physico-Mechanical Institute of the NAS of Ukraine. Naukova Str., 5, Lviv-79060, Ukraine. E-mail: kristinavlad1998@gmail.com

2 Chuiko Institute of Surface Chemistry, NASU, 17 General Naumov Str., Kyiv 03164, Ukraine.

Metallic nanoparticles of Ni and Co are of great interest due to features of their magnetic and catalytic properties arising from a small size and high specific surface area [1]. They are used also as binders for the negative MH-electrode preparation of Ni-MH batteries. Metallic powders reduce the internal resistance of the electrodes, provide electrical contact and thus help increase the discharge capacity and improve the reversibility of charge-discharge processes. It should be note that some of Ni/Co-based nanomaterials possess its own high electrochemical capacity and can be effectively used for preparation of MH-electrodes.

Nickel and/or cobalt carbon nanoparticles were synthesized from polystyrene and metal salts using pyrolysis method [2]. The morphology, structural features and electrochemical hydrogenation properties of the obtained nanomaterials were investigated by scanning electron microscopy, X-ray powder diffraction, galvanostatic charging-discharging, volt- and chrono-amperometry. The crystallinity of the synthesized Ni/Co-C nanoparticles was confirmed by the X-ray diffraction. Ni/Co-C composites were obtained by mixing with carbonyl nickel, pressed into pellets. Electrochemical parameters (discharge capacity and cyclic stability) were studied and their substantial dependence from the Ni/Co ratio was shown. The obtained results will be analyzed and compared with those for Ni-Co nanoparticles synthesized by other methods.

- Kytsya A., Berezovets V., Verbovytskyy Yu., et. al. Bimetallic Ni-Co nano-particles as an efficient catalyst of hydrogen generation via hydrolysis of NaBH4 // J Alloys Compd.-2022.-908.-P.1-9 [164484].

- Galaburda M., Bogatyrov V., Oranska O., et. al. Synthesis and characterization of carbon composites containing Fe, Co, Ni nanoparticles // J Therm Anal Calorim. - 2015.-5.-P. 553-561.