Nanocomposites and nanomaterials
Investigation of Nanodiamonds for NMR relaxometry sensors application

 Y.S. Milovanov1, I.V. Gavrilchenko1, I.I. Ivanov1,O.V.Kozinetz, V.V.Lysenko2, V.A. Skryshevsky1
1 Institute of High Technologies, Taras Shevchenko National University of Kyiv, 01601 Volodymyrska str. 64, Kyiv, Ukraine.
E-mail: ir.gavril11@gmail.com
2 Université Claude Bernard Lyon 1disabled, Villeurbanne, France.

Nanodiamonds (ND) are a separate class of nanoparticles in the carbon family. These nanoparticles are usually 1 to 100 nm in size and are produced by synthesis based on the detonation of a carbonaceous explosive. Different processing conditions, processing technologies and production methods create different surface properties, which leads to different types of ND, which differ in surface chemical composition, structure, shape and size.
The ND structure can be represented in a core-shell model in which the core (diamond carbon) is inert, while the surface shell is partially based on graphite, which allows to add various functional groups, such as carboxyl or hydroxyl, which will determine the properties of ND [1]. Therefore, they can be used as a delivery system for a huge range of drugs, antigens and antibodies. On the other hand, their spectroscopic properties make them ideal for in vivo imaging [1], especially for the diagnosis of specific target cells, increasing the sensitivity of the current therapeutic or diagnostic imaging. We used ND to alter the relaxation of nuclear spins, which is based on the NMR technique used to detect molecules. Nuclear magnetic resonance (NMR) is a powerful magnetic phenomenon that can be used toidentify, image, and detect molecules [2].The relaxation time in different alcohol solutions was measured. The results of the experiment show that the relaxation time T1 slightly (slightly) decreases with increasing concentration of water in alcohol. With the addition of nanodiamonds, the situation changes significantly, there is a sharp drop in relaxation time for all types of alcoholic beverages, depending on the concentration of water-spray solution.
1. Jin-Xu Qin et al., ‘Nanodiamonds: Synthesis, properties, and applications in nanomedicine’, Materials & Design,V. 210, 2021, 110091, ISSN 0264-1275, https://doi.org/10.1016/j.matdes.2021.110091.
2. R. Austin et al., ‘MagViz: A Bottled Liquids Scanner Using Ultra-Low Field NMR Relaxometry’, in Magnetic Resonance Detection of Explosives and Illicit Materials, T. Apih, B. Rameev, G. Mozzhukhin, and J. Barras, Eds. Dordrecht: Springer Netherlands, 2014, pp. 99–110. doi: 10.1007/978-94-007-7265-6_9.