Nanocomposites and nanomaterials

Catalytic activity of composites of nickel boride nanoparticles and anodic nanoporous alumina in hydrogenation reactions
Lytvynenko A.S.1,2, Mishura A.M.1, Kurmach M.M.1, Brzózka A.3, Zaraska L.3
1 Porous Compounds and Materials Dept., L. V. Pisarzhevskii Institute of Physical Chemistry of the NAS of Ukraine. Prospect Nauky, 31, Kyiv, 03028, Ukraine.
E-mail: anton.s.lytvynenko@gmail.com
2 Charles University, Faculty of Science, Department of Analytical Chemistry, Albertov 6, 128 00 Prague 2, Czech Republic
3 Jagiellonian University, Faculty of Chemistry, Gronostajowa 2, 30-387 Kraków, Poland.

Hydrogenation is an important process for organic synthesis leading to valuable chemicals for pharmaceutics and agrochemistry [1]. Ni-based nanoparticles (NPs) are promising substitutes for Pd catalysts typically employed for such reactions. Immobilization of NPs on a porous support improves their separation from the reaction mixture, mitigates their aggregation etc. The work aimed at assessment of the catalytic activity of Ni boride NPs immobilized on anodic nanoporous alumina (AAO) in hydrogenation of heteroaromatic compounds on an example of a substituted imidazo-[1,5-a]-pyridine S (Fig. 1).
Fig. 1: The compound S.
The AAO samples were prepared by the two-step anodization of Al, as reported previously by us. Ni boride NPs were applied via treatment with NiCl2 solution followed by reduction with NaBH4. The hydrogenation of S was performed in CH3OH by NaBH4 or gaseous H2 (1 atm). The keto-group of S, its pyridine ring or both groups could be affected. Both NaBH4 and H2 together with the obtained composites resulted in hydrogenation of both S groups, contrary to H2 on Pd/C catalysts (yielding the mixture of all possible products). The composites exhibited notably higher activity than Ni boride without the support.
The authors thank to Ms. Karolina Podsiadło and Mr. Kacper Motyka for their assistance in samples preparation. The work was supported by the joint Polish-Ukrainian scientific project co-funded by the Ministry of Education and Science of Ukraine (contracts Nos M/115-2020 and M/110-2021) and Polish National Agency for Academic Exchange (contract No PPN/BUA/2019/1/00034/U/00001).

Duan Y., Li L., Chen M.-W., Yu Ch.-B., Fan H.-J., Zhou Y.-G. Homo­genous Pd-Catalyzed Asymmetric Hydrogenation of Unprotected Indoles: Scope and Mechanistic Studies // J.Am.Chem.Soc.-2014.-136.-P.7688-7700.