Photonic properties of hybrid liquid crystal cells with artificial opals

O. Perederii, S. Bugaychuk, A. Iljin, L. Tarakhan, A. Negriyko
Institute of Physics of NASU, Kiev, Ukraine

One of the priority directions of the fundamental nanoscience is the use of various nano- and micro-structured surfaces to enhance the physical properties of materials, including optical, electrical and others. The material and devices of nonlinear photonics are of great interest for use as new technologies and in optical communication systems in the near future. We are investigating hybrid liquid crystal (LC) cells containing a substrate coated with an artificial opal film. The opal is a periodic packaging of silica crystal spheres. Opal films have been grown in a glass substrate. We have obtained various types of opal films: an artificial crystalline opal with a periodic crystal structure of SiO2, and amorphous films that show no regular periodic structure. We have characterized these films with atomic force microscopy (AFM) and high resolution optical microscopy. We also have investigated their optical characteristics, such as the anisotropy of optical diffraction.
A conventional hybrid LC cell consists of a glass substrate coated with a transparent ITO conductive film, a substrate with a heterogeneous conductive surface, and an LC layer between them. The LC layer makes it possible to enhance the photorefractive nonlinear-optical response, which is photoinduced on a conductive heterogeneous surface on which an electric field is applied [1-2]. Since the film of artificial opal does not conduct electricity, we manufactured hybrid LC cells with planar electrodes, that is, the electrodes were placed between the substrates and served as spacers. The research of nonlinear optical response in such cells have been carried out. Mechanisms of optical nonlinearity and methods for its control in such cells containing heterogeneous opal film are being developed. This way, hybrid LC cells with an opal film are of interest for studying the intrinsic mechanism of bonding of LC molecules with a heterogeneous surface.

[1] P.P. Korneychuk, O.G. Tereshchenko, Yu.A. Reznikov, V.Yu. Reshetnyak, K.D. Singer, Hidden surface photorefractive gratings in a nematic-liquid crystal cell in the absence of a deposited alighment layer, J. Opt. Soc. Am. B, 23 (6), p. 1007 (2006).
[2] S. Bugaychuk, A. Iljin, O. Lytvynenko, L. Tarakhan, L. Karachevtseva, Enhanced nonlinear optical effect in hybrid liquid crystal cells based on photonic crystal, Nanoscale Research Letters, 12:449, 1-9 (2017).