Nanostructured surfaces

Arrays of nanotips on Si(001) formed in high vacuum through thermally stimulated surface diffusion enhanced by electric field
Goriachko A.M.1
1 Department of Physical Electronics, Radiophysics Faculty, National Taras Shevchenko University of Kyiv. Glushkova 4G, Kyiv-03187, Ukraine.
E-mail: andreandy2000@gmail.com

Experimental procedures required to obtain an atomically clean and atomically flat silicon surface had been exhaustively documented and widely reproduced. Typically it takes numerous cycles of rapid annealing up to ~1200°C in ultra-high vacuum environment, yielding Si(001), Si(111), etc. surfaces composed of flat terraces separated by steps of atomic height. Technically, sending electric current through the silicon sample is the simplest and mostly “traditional” way to achieve the required preparation temperature. More exotic (and complicated) options include laser radiation, heat transfer through a direct contact, various types of furnaces and subjecting the sample to charged particle beams.
In the present work, the Si(001) surface was annealed in high vacuum at 1200°C for several minutes by means of electron bombardment of the back side of the sample. The electrons were emitted from the W cathode (direct current heated) at ground potential, while the Si sample was kept at +3 kV. After cooling to room temperature the samples were investigated by means of atomic force microscopy (AFM) in an ambient environment. Figure 1 shows the typical surface morphology after the above described preparation procedure.

Figure 1. Grey scale AFM image of the Si(001). Field of view is 10×10 mkm2. To the right from the image is the height-distance cross-section taken along the white fine-dashed line.