### Nanocomposites and nanomaterials

Estimation of thermal diffusivity of expanded graphite - carbon nanotubes composites by heat pulse and thermo-wave methods

Morozovsky N.V 1, Barabash Yu.M.1, Dovbeshko G.I.1,

Grebelna Yu.V.2, Kartel M.T.3, Sementsov Yu.І.3

1 Institute of Physics, NAS of Ukraine, 03028 Kyiv, Ukraine.Prospect Nauki, 46, Kyiv-03028, Ukraine.

E-mail: nicholas.v.morozovsky@gmail.com

2 TM Spetsmash ltd., 02094, Viskozna str., 5, Kyiv, Ukraine.

3 O. Chuiko Institute of Surface Chemistry, NAS of Ukraine, 03164, Kiev, Ukraine.

Carbonaceous materials possess large application spectrum from nano-technologies to bio-sensorics, medicine and thermal management. In particular, carbon nanotubes based composite was proposed as thermal absorber for pyroelectric and other thermal detectors [1].

Thermal diffusivity aT is the thermophysical parameter determining the speed of temperature front propagation during pulse or periodic variations of the temperature distribution in a medium.

The sheet samples of thermally expanded graphite (EG) - carbon nanotubes (CNT) composites(c) were synthesised by persulphate oxidation method [2]. In both heat pulse method and thermo-wave probing of (EG-CNT)c, the light emitting diode as radiation heater and the pyroelectric detector as heat sensor were utilised.

Obtained by heat pulse method aT values of (EG-CNT)c are (2 - 8)∙10-6 m2/s and by thermo-wave probing are (1.5 - 16)∙10-5 m2/s, and lie in the range limited by aT values known for CNT-mats (~ 10-6 m2/s) and for isolated CNT (~ 10-2 m2/s).

- Bravina S. L., Morozovsky N. V., Dovbeshko G. I., Fesenko O. M., Obraztsova E. D. Carbon nanotubes based black absorbing coatings for pyroelectric and other thermal detector application // Nanosystems, Nanomaterials, Nanotechnologies.-2009.-7, N 1.-P. 137-145.

- Sementsov Yu. I., Pyatkovsky M. L., Cartel M. T., Kozik O. Ya., Gozhjinsky S. M., Zhang W., Zhou G., Zhang X., Li Z., Liu H., Zheng L.W., Zhang Y., Wang S., Zhang S., Wei J. Method for obtaining intercalated graphite and device for its implementation // Patent of Ukraine for invention No. 111407. April 25.-2016. Bull N. 8.