### “Nanochemistry and biotechnology”

Electrochemical synthesis of silver nanoparticles using surfactants of glycolipid nature

O.I. Kuntyi1, O.V. Karpenko2, A.R. Kytsya2, G.I. Zozula1, A.S. Mazur1

1Lviv Polytechnic National University,

12 Bandera Str., Lviv 79013, Ukraine.

E-mail: kunty@ukr.net

2Department of Physical Chemistry of Fossil Fuels InPOCC,

NAS of Ukraine, 3а Naukova Str., Lviv, 79053, Ukraine

In the last years, the interest in the electrochemical obtaining of colloid solutions of silver nanoparticles (AgNPs) has significantly increased due to their possibility of controlling and green synthesis [1]. To ensure the latter, it is advisable to use natural precursors, promising ones are ecologically safe surfactants of glycolipid nature, in particular rhamnolipids [2].

The paper reports on electrochemical synthesis of colloidal AgNPs solutions involving the reverse electrolysis mode and silver electrodes. Rhamnolipids and rhamnolipid biocomplex have been used as stabilizers. The recorded UV/Vis spectra of AgNPs solutions indicate the presence of an absorption band with maximum in 420-430 nm. As the results shown, the sizes of the obtained silver nanoparticles were 10 ± 5 nm (Fig.1).

|  | Fig.1 TEM image of AgNPs prepared from solution of rhamnolipid (1 g·l-1) at 50 oC by reverse electrolysis mode |
| --- | --- |

The effect of the stabilizer concentration, electrolysis voltage and temperature on the size of the nanoparticles and the rate of the process have been established.

- Thuc D.T., Huy T.Q., Hoang L.H. et al. Green synthesis of colloidal silver nanoparticles through electrochemical method and their antibacterial activity // Mater. Lett. – 2016. – V. 181. – P. 173-177.

- Kłosowska-Chomiczewska, I.E., Mędrzycka, K., Hallmann, E., Karpenko et al. Rhamnolipid CMC prediction // J. Colloid Iinterface Sci. – 2017. – V. 488. – Р. 10-19.