Nanocomposites and Nanomaterials

The Thin Film Thickness Effect on the Properties of In2O3

T. Asar1,2,*, H. İ. Efkere2, C. Başköse2, Y. Özen1,2, S. Özçelik1,2
1 Physics Department, Faculty of Sciences, Gazi University, 06500, Ankara, Turkey
2 Photonic Application and Research Center, Gazi University, 06500, Ankara, Turkey
* Corresponding Author: trkasar@gazi.edu.tr

Indium Oxide (In2O3) thin films have been extensively studied as a n-type semiconducting binary oxide material, which has wide band gap, high electrical conductivity, high optical transparency and high carrier transport capability [1–3]. It was also seen that the properties of such thin films can be enhanced with adjusting the deposition parameters [4]. Therefore, in this study, the effects of thin film thickness were investigated for In2O3 thin films.

The un-doped In2O3 thin films were deposited on the n-type Si (100) substrate by RF magnetron sputtering technique. 100W RF power was used for the deposition of the In2O3 thin films which have 100 nm (IO-1), 150 nm (IO-2) and 200 nm (IO-3) thicknesses. After the deposition processes, the structural and optical properties of the samples were determined by X-Ray Diffraction (XRD), and Ultraviolet-Visible (UV-Vis) spectrometer measurements.

The XRD measurements showed that the In2O3 thin films have Si (400), In2O3 (631), In2O3 (543), In2O3 (640), In2O3 (721) and In2O3 (642) diffraction peaks. That means, the deposited thin films have polycrystalline structure. The band gap values which were consistent with the literature [5,6] were extracted from the (α*hν)2-Photon Energy graph as 3,75 eV (IO-1), 3,87 eV (IO-2) and 3,93 eV (IO-3). Thus, it can be said that the structural and optical properties of the In2O3 were affected from the thin film thickness.

Acknowledgments:	This study is supported by the Ministry of Development of Turkey under project numbers: 2011K120290 and 2016K121220.

[1]	T. Asar, B. Korkmaz, H.İ. Efkere, N. Akin, S. Özçelik, Investigation of the structural, morphological, optical and electrical properties of In2O3 thin films: Gas sensor applications, J. Polytech. 21 (2018) 265–271.
[2]	M.A. Islam, M. Nuruzzaman, R.C. Roy, J. Hossain, K.A. Khan, Investigation of Electrical and Optical Transport Properties of N-type Indium Oxide Thin Film, Am. J. Eng. Res. 4 (2015) 62–67.
[3]	H.I. Yeom, J.B. Ko, G. Mun, S.H.K. Park, High mobility polycrystalline indium oxide thin-film transistors by means of plasma-enhanced atomic layer deposition, J. Mater. Chem. C. 4 (2016) 6873–6880.
[4]	M.D. Giulio, G. Micocci, A. Serra, A. Tepore, R. Rella, And, P. Siciliano, Characteristics of reactively sputtered Pt-SnO2 thin films for CO gas sensors, J. Vac. Sci. Technol. A. 14 (1996) 2215–2219.
[5]	A. Ayeshamariam, M. Bououdina, C. Sanjeeviraja, Optical, electrical and sensing properties of In2O3 nanoparticles, Mater. Sci. Semicond. Process. 16 (2013) 686–695.
[6]	M. Jothibas, C. Manoharan, S. Ramalingam, S. Dhanapandian, S. Johnson Jeyakumar, M. Bououdina, Preparation, characterization, spectroscopic (FT-IR, FT-Raman, UV and visible) studies, optical properties and Kubo gap analysis of In2O3 thin films, J. Mol. Struct. 1049 (2013) 239–249.