Physico-Chemical nanomaterials science

Modification of the strain state and analysis of crystalline changes in the ion implanted AlN/GaN superlattices
Liubchenko O.I., Sabov T.M., Melnik V.P.  Kladko V.P., Romanyuk B.M. , Yukhymchuk V.О., Kolomys O.F., Dubikovskyi O.V. ,Gudymenko O.Yo., Belyaev A.E.
1 V. Lashkaryov Institute of Semiconductor Physics, National Academy of Sciences of Ukraine, Pr. Nauky 41, 03028 Kiev
E-mail: lubchenco.a@gmail.com

3-nitride compounds (AlxGa1-xN) are widely used as the active layers in light emitting diodes, laser diodes and hight-electron mobility transistors. Thickness fluctuation of barriers and quantum well (QW) layers in superlattices (SL) as well as mechanical stresses can lead to significant changes in their functional characteristics [1]. Therefore, the advancement of previously reported methods [2] and the development of new approaches for controlling the strain state in such systems is important for practical application.
In this work, we investigate the strain distribution and the emission properties of implanted by Ar ions GaN/AlN SL. The X-ray diffraction 2θ-ω scans of 0002 reflection from SL before and after implantation have been measured and modeled using the developed software. The simulation of the spectra provided the dislocation densities, depth profiles of thickness variation and of strain distribution. The simulation has showed that the implantation affects the relaxation of the AlN barriers and the strain of GaN QW only down to a certain depth of the SL. The analysis of room-temperature photoluminescence spectra shows the strain value of ε = 0.0031, which is close to that obtained from XRD (ε = 0.0028). The Secondary-ion mass spectrometry indicated changes in the sputtering rate before and after implantation.

1. A. Kaminska , P. Strak, J. Borysiuk, K. Sobczak, J. Z. Domagala, M. Beeler, E. Grzanka, K. Sakowski, S. Krukowski, and E. Monroy. Correlation of optical and structural properties of GaN/AlN multi-quantum wells—Ab initio and experimental study // J. Appl. Phys.-2015.-119.-P. 015703.
2. B. Romanjuk, V. Kladko, V. Melnik, V. Popov, V. Yukhymchuk, A. Gudymenko, Ya. Olikh, G. Weidner, D. Kruger. Enhanced relaxation of SiGe layers by He + implantation supported by in situ ultrasonic treatments. // Materials Science in Semiconductor Processing.-2005.-8.-P. 171–175.